Novel C5 Resins

NEVTAC® T950 & T1000

Description

NEVTAC® T950 and T1000 are thermoplastic, low molecular weight hydrocarbon resins made through the

polymerization of mixed DCPD and aliphatic monomers. Primary uses include pressure-sensitive adhesives,

hot melt adhesives, coatings and rubber compounding. They serve as functional alternatives to traditional

piperylene-based and aromatic-modified C5 resins. These resins offer a strong balance of tack, adhesion, co-

hesion, along with good heat resistance, broad compatibility and solubility.

| Applications | Compatible Systems | Features |
| --- | --- | --- |
| Hot Melt | SBC (SBS, SIS, SEBS) | Tack Build |
| Pressure Sensitive Adhesives | EVA | Hydrophobic |
| Tire and Rubber | Polyolefins | Resistant to Acids and Alkalis |
| Elastomeric Sealants | Butadiene Rubber | Adhesion Promoter |
| Water resistant coatings | Butyl Rubber | Good Compatibility |
| Asphalt Modification | Natural Rubber | Low Molecular Weight |

Typical Properties

| Properties | Test Method | NEVTAC® 100 | Super NEVTAC® 99 | NEVTAC® T950 | NEVTAC® T1000 |
| --- | --- | --- | --- | --- | --- |
| Basic Chemistry | - | Piperylene | Aromatic modified Piperylene | Modified DCPD | Modified DCPD |
| Softening Point, R&B °C | ASTM E28 | 100 | 95 ± 3 | 92 ± 3 | 100 ± 5 |
| Gardner Color (50% in Solvent) | ASTM D1544 | 3.5 | 4.5 | 9.0 | 9.0 |
| Specific Gravity @ 25 °C | ASTM D71 | 0.97 | 0.97 | 1.08 | 1.08 |
| Viscosity Brookfield, cps 140 °C 160 °C 180 °C | ASTM D3236 | 6,050 1,300 400 | 3,700 860 290 | 2,700 600 200 | 7,300 1,300 400 |
| Molecular Weight Mn Mw | ASTM D5296 | 1,150 2,800 | 1,000 2,300 | 390 800 | 390 800 |
| Appearance | Visual | Pale yellow pellets | Pale yellow pellets | Yellow flakes | Yellow flakes |

*Typical properties are not constructed as specifications.

Novel C5 Resins

NEVTAC® T950 & T1000

| Function | Component | SIS PSA | SBS PSA |
| --- | --- | --- | --- |
| SIS Elastomer | Kraton D-1161 | 17.5 | / |
| SBS Elastomer | Kraton D-1101 | / | 10 |
| Tackifier | NEVTAC® T1000 NEVTAC® 100 Super NEVTAC® 99 | 26.5 | 25 |
| Oil | Calsol 5550 | 6 | 15 |
| Antioxidant | BNX 1010 | 0.25 | 0.25 |
| Solvent | Toluene | 50 | 50 |

Performance in Pressure Sensitive Adhesives

*Score displayed on charts was indexed to NEVTAC® 100 as a benchmark.

Performance of NEVTAC® T1000 was observed in a SIS system. Tack, heat resistance and peel strength all performed comparable to a piperylene-based C5 Resin.

Performance of NEVTAC® T1000 was observed in a SBS system. Tack, heat resistance and peel strength all performed significantly better compared to a piperylene-based C5 Resin.

Performance of NEVTAC® T1000 was observed in both SBS and SIS systems. In the SBS system, tack, heat resistance, and peel strength showed significant improvement compared to a piperylene-based C5 resin. In the SIS system, these properties performed comparably to the piperylene-based C5 resin.

Performance in Hot Melt Adhesives

| Compatibility (Cloud Points) °C | NEVTAC® 100 | Super NEVTAC® 99 | NEVTAC® T1000 |
| --- | --- | --- | --- |
| Elvax 40 (40% VA) | >170 | >170 | >170 |
| Elvax 150 (33% VA) | 160 | 135 | 105 |
| Elvax 250 (28% VA) | 125 | 95 | N/A |
| Elvax 410 (18% VA) | 60 | 60 | 55 |

*NEVTAC® T1000 showed comparable compatibility with EVA and Wax.

April 2026

Compatibility is evaluated using an EVA/resin/wax ratio of 1:1:1. The cloud point test shows the temperature at which the system exhibits cloudiness; the lower number indicates better compatibility between the resin and the EVA/wax system.